3-Part CSI MasterFormat Specification

SECTION 08 3483

Floor DOORs AND FRAMES

GENERAL

SUMMARY

Section includes:

Floor Doors for access between building floors as indicated on drawings and specified herein

references

Aluminum Diamond Tread Plate:  ASTM B632-02, 1/4 inch 6061-T6 aluminum with mill finish.

Aluminum Extrusion:  6061-T6 aluminum.

Steel Diamond Tread Plate:  ASTM A786.

Steel Angle:  ASTM A36-94 steel frame, structural.

Stainless Steel Diamond Tread Plate:  ASTM A793 stainless steel, No. 304 finish.

Stainless Steel Angle:  ASTM A276 stainless steel, No. 304 finish.

Stainless Steel Smooth Plate:  ASTM A240 smooth plate stainless steel, type No. 316.

Fasteners:  Type No. 316 stainless steel.  ASTM F593 for bolts and ASTM F594 for nuts.

General:  Comply with NAAMM's "Metal Finishes Manual for Architectural and Metal Products" for recommendations for applying and designating finishes.

SUBMITTALS

Shop Drawings: Indicate configuration and dimensions, show components, adjacent construction, required clearances and tolerance and other affected work.

Product Data:  Manufacturer’s technical data for each type of floor door, including setting drawings and finish requirements

Manufacturer's Installation Instructions and Operation & Maintenance:  Indicate installation, operation and maintenance requirements and rough-in dimensions.

Quality Assurance

Qualifications:

Manufacturer/Installer:  Company specializing in manufacturing and installation of components specified in this Section with minimum of 5 years documented experience.

Regulatory Requirements:

International Building Code for fire resistance rated construction

IBC Section 712 for Floor Fire Doors- tested in accordance with NFPA 288 and labeled by approved agency; Warnock Hersey or Underwriters Laboratory.

DELIVERY, STORAGE, and HANDLING

Deliver materials to Project site ready to use.

Exercise proper care in handling of Work so as not to disrupt finished surfaces.

Store materials under cover in a dry and clean location off the ground.

WARRANTY

Provide manufacturer's standard warranty.  Floor doors shall be free from manufacturing defects in materials and fabrication for a period of 5 years from the date of shipment.  Should a product fail to function in normal use within this period, manufacturer shall furnish a replacement or new part at Nystrom’s discretion

PRODUCTS

MANUFACTURER

Nystrom

9300 73rd Ave N

Minneapolis, MN  55428

PH: 800-547-2635

www.Nystrom.com

FIRE-RATED ALUMINUM FLOOR DOORS

        - Fire-Rated Aluminum Floor Door. Model FC

Clear Unobstructed Opening Size: <Insert dimensions>.

Frame: 1/4 inch (6.4 mm) mill finish aluminum plate with epoxy on exterior frame, angle profile.[Frame with 3/8 inch (9.5 mm) holes for bolt in] [Frame with integral masonry anchors for cast-in-place].

Door: Single leaf; 1/4-inch-thick (6.4-mm-thick) aluminum diamond tread plate with 3 layers of Endothermic E-5A Mat, and 3 inch thick (76 mm thick) 3M Duct Wrap blanket.

Loading Capacity: 300-lbf/sq. ft. (14.4-kN/sq. m) pedestrian live load and a maximum deflection of 1/150 of span.

Fire Rating: Maintains a [2 hour fire rating; Model FCRM] [3 hour fire rating; Model FCCM] for floor/ceiling assembly as tested and labeled by Warnock Hersey according to NFPA 288.

Options:

- Self-Closing Mechanism; Automatically closes door at 165 deg F (74 deg C) in event of fire, dampers for slow opening.

Hardware:

  - Material and Finish: Type 316 stainless steel, including latch and lifting mechanism assemblies, hold-open arms, and brackets, hinges, pins, and fasteners.

  - Hinges: 3 inch by 3 inch (76 mm by 76 mm) type 3/16 heavy-duty butt hinge with stainless-steel pin fastened to door with stainless steel carriage bolts.

  - Operating Mechanism: Type 316 stainless steel gas springs.

  - Latch: Stainless-steel slam latch with internal pull release cable and outside removable square L handle.

  - Anchor 4 inch (102 mm) concrete anchor straps provided

Fire-Rated Aluminum Floor Door with Recessed Cover: Allows for flooring infill. Model FT

Clear Unobstructed Opening Size: <Insert dimensions>.

Frame: 1/4 inch (6.4 mm) mill finish aluminum recessed for 1/8 inch (3.2 mm) flooring infill.[Frame with 3/8 inch (9.5 mm) holes for bolt in] [Frame with integral masonry anchors for cast-in-place].

Door: Single leaf; 1/4-inch-thick (6.4-mm-thick) aluminum plate.

Insulation: 3 layers of Endothermic E-5A Mat, and 3 inch thick (76 mm thick) 3M Duct Wrap blanket.

Loading Capacity: 300-lbf/sq. ft. (14.4-kN/sq. m) pedestrian live load and a maximum deflection of 1/150 of span.

Fire Rating: Maintains a [2 hour fire rating; Model FTRM] [3 hour fire rating; Model FTCM] for floor/ceiling assembly as tested and labeled by Warnock Hersey according to NFPA 288.

Option:

            - Self-Closing Mechanism: Automatically closes door at 165 deg F (74 deg C) in event of fire, dampers for slow opening.

Hardware:

  - Material and Finish: Type 316 stainless steel, including latch and lifting mechanism assemblies, hold-open arms, and brackets, hinges, pins, and fasteners.

  - Hinges: 3 inch by 3 inch (76 mm by 76 mm) type 3/16 heavy-duty butt hinge with stainless-steel pin fastened to door with stainless steel carriage bolts.

  - Operating Mechanism: Type 316 stainless steel gas springs.

  - Latch: Stainless-steel slam latch with internal pull release cable and outside removable square L handle.

Safety Accessories: Safety [grate] [chains] [net] [railing] [telescoping safety post] <Insert safety device>.

EXECUTION

EXAMINATION

Verify that preparation and affected dimensions are acceptable.

Verify tolerances and correct improper conditions.

PREPARATION

Advise installers of details relating to floor hatch installation, including rough opening dimensions, locations of supports, and anchoring methods.

INSTALLATION

Follow manufacturer’s instructions for installing floor doors and hatches.

Install frames plumb and level in opening, in proper alignment with floor surface for flush installation.  Secure rigidly in place.

Position units to provide convenient access to concealed Work requiring access.

ADJUSTING

Operational Units:  Test-operate units with operable components.

Clean and lubricate joints and hardware.

Adjust for proper operation.

CLEANing

Clean adjacent surfaces and remove unused product and debris from site.

Adjust doors for smooth operation.

END OF SECTION

Rev 01/19